# Product Information

Copper Phosphorus CP3 Brazing Rods
Brand: Super 6

Product Description

Super 6 CP3 Brazing Rods are high-phosphorus, deoxidised copper rods designed for gas brazing and welding of copper and copper-based alloys. With excellent flow characteristics and a low melting point, CP3 rods produce sound, leak-free joints ideal for plumbing, heating, refrigeration, and electrical systems. Thanks to their self-fluxing properties on copper, these rods eliminate the need for additional flux in many copper brazing applications, simplifying the process and improving reliability.

Key Features

- High-phosphorus copper alloy for smooth flow and capillary brazing

- Self-fluxing on copper joints – no additional flux needed

- Low melting range reduces heat input and risk of base metal distortion

- Produces clean, reliable, and leak-proof joints suitable for pressure and thermal cycling

- Supplied in convenient 1kg tube packs for workshop or site use

Typical Applications

- Plumbing and central heating installations

- Refrigeration and air conditioning systems

- Electrical conductor and motor coil connections

- General copper and copper alloy brazing

- Leak-proof pipe and tube assemblies

Chemical Composition (% by weight)

| Element | Typical Content |
| --- | --- |
| Copper (Cu) | Approx. 97 – 98% |
| Phosphorus (P) | Approx. 1.0 – 1.3% |
| Other | ≤ 0.5% |

## Physical and Technical Data

| Property | Value |
| --- | --- |
| Melting Range | Approx. 680 – 780°C |
| Recommended Brazing Temperature | 660 – 760°C |
| Flux Type | Bare rod (self-fluxing on copper) |
| Suitable Brazing Methods | Oxy-acetylene, torch |
| Joint Strength | High, leak-proof joints |

## Safety and Handling

- Use in well-ventilated areas to avoid inhaling fumes

- Always wear appropriate PPE, including gloves and safety goggles

- Follow all applicable health and safety regulations during use

Liability Notice: Whilst all reasonable efforts have been made to ensure the accuracy of the information contained, this information is subject to change without notice and can be only considered as suitable for general guidance.